Harsh Chauhan

23321014

TEB – 103

ETE

| Material | project Id | space group |
| --- | --- | --- |
| NiO | mp-19009 | Fm3̅m |
| CoO | mp-22408 | F4̅3m |
| FeO | mp-1274279 | C2/m |
| TiO2 | mp-390 | I4₁/amd |
| RuO2 | mp-825 | P4₂/mnm |
| IrO2 | mp-2723 | P4₂/mnm |
| SrTiO3 | mp-5229 | Pm3̅m |
| LaMnO3 | mp-17554 | Pnma |

b)

To quantitatively isolate and measure the D3-induced error, the following protocol was used:

Step 1: Selection of optimized structure

The optimized crystal structures of all eight transition metal oxides were obtained from the Materials Project database.

Step 2: Uniform lattice expansion

Each crystal structure was uniformly expanded by applying strain to the lattice parameter:

ai=a0(1+si)

where:

- a0= original lattice parameter

- si= applied strain

- ai= strained lattice parameter

Step 3: D3 dispersion energy calculation

For every strained structure, the D3 dispersion energy Ediswas calculated and recorded.

Step 4: Plotting dispersion-energy curve

A graph of:

Edis  vs  Cell Length

was plotted for each material.

Step 5: Identification of dip

The abnormal minimum point (dip) in the curve was identified:

Emin

This point corresponds to the strongest artificial lowering of D3 energy.

Step 6: Estimation of smooth baseline

A smooth baseline was constructed by connecting the pre-dip shoulder and post-dip recovered region:

Eexpected(x)=mx+b

where:

m=ER-ELxR-xL
b=EL-mxL

Step 7: Calculation of D3-induced error

The D3-induced error was calculated as:

ΔE=Emin-Eexpected,dip

where:

- Emin= observed minimum dispersion energy

- Eexpected,dip= expected smooth energy at dip position

Magnitude:

∣ΔE∣

represents the strength of D3-induced error.

Figure: Representative dispersion-energy vs cell length plot showing pre-dip shoulder, artificial D3 dip Emin, and recovered post-dip region used for baseline fitting.

c)

The D3-induced error contribution was extracted for all eight transition metal oxides using the local peak-dip-recovery baseline method. The error was calculated using:

ΔE=Emin-Eexpected,dip

where Eminis the observed minimum dispersion energy at the dip point, and Eexpected dipis the expected smooth baseline energy at the same position. The magnitude ∣ΔE∣represents the D3-induced error contribution.

| Material | Material Project ID | Space Group | Dip Cell Length | Emin | Eexpected,dip | ΔE | ∣ΔE∣ |
| --- | --- | --- | --- | --- | --- | --- | --- |
| NiO | mp-19009 | Fm3̅m | 3.204498 | -0.031086 | -0.012859 | -0.018227 | 0.018227 |
| CoO | mp-22408 | F4̅3m | 3.468908 | -0.042808 | -0.019069 | -0.023739 | 0.023739 |
| FeO | mp-1274279 | C2/m | 2.720810 | -0.091038 | -0.046713 | -0.044324 | 0.044324 |
| TiO2 | mp-390 | I4₁/amd | 5.144189 | -0.033192 | -0.013372 | -0.019820 | 0.019820 |
| RuO2 | mp-825 | P4₂/mnm | 3.422476 | -0.047043 | -0.038392 | -0.008651 | 0.008651 |
| IrO2 | mp-2723 | P4₂/mnm | 4.288553 | -0.033895 | -0.030374 | -0.003522 | 0.003522 |
| SrTiO3 | mp-4651 | Pm3̅m | 7.174065 | -0.100512 | -0.038759 | -0.061753 | 0.061753 |
| LaMnO3 | mp-17554 | Pnma | 8.513574 | -0.222176 | -0.089542 | -0.132634 | 0.132634 |

From the table, LaMnO₃ has the largest D3-induced error contribution, while IrO₂ has the smallest. The overall order of error magnitude is:

LaMnO3>SrTiO3>FeO>CoO>TiO2>NiO>RuO2>IrO2

d)

The calculated D3-induced error magnitudes follow the order:

LaMnO3>SrTiO3>FeO>CoO>TiO2>NiO>RuO2>IrO2

This trend indicates that D3-induced error depends strongly on structure type, ionic size, oxidation state, packing density, and electronic/geometric distortions.

Table 1: Summary of D3-induced error trend

| Material | Structure Type | ∣ΔE∣ | Key Reason for Trend |
| --- | --- | --- | --- |
| LaMnO₃ | Distorted Perovskite | 0.132634 | Large La ion + Jahn–Teller distortion + open structure |
| SrTiO₃ | Perovskite | 0.061753 | Large Sr ion + extended TiO₆ network |
| FeO | Distorted Rock Salt | 0.044324 | Lower symmetry + distorted Fe–O coordination |
| CoO | Rock Salt | 0.023739 | Moderate ionic packing |
| TiO₂ | Oxide Network | 0.019820 | Relatively regular TiO₆ arrangement |
| NiO | Rock Salt | 0.018227 | Compact symmetric ionic lattice |
| RuO₂ | Rutile | 0.008651 | Dense packing + smooth coordination change |
| IrO₂ | Rutile | 0.003522 | Most compact regular structure |

Effect of structure type

Perovskite oxides show the highest D3-induced errors because they contain multiple coordination environments, large cation sites, and extended octahedral frameworks. During expansion, many weak long-range interactions change simultaneously, producing a stronger artificial dip.

Rock salt oxides show moderate error because their packing is compact and coordination is simpler.

Rutile oxides show the smallest error due to dense packing and regular octahedral arrangement, which keeps D3 variation smooth.

Table 2: Critical factors affecting D3-induced error

| Factor | Effect on D3-induced Error | Example |
| --- | --- | --- |
| Large ionic size | Increases polarizability → increases error | La³⁺, Sr²⁺ |
| Open crystal packing | More weak long-range interactions | Perovskites |
| Structural distortion | Causes abrupt coordination change | LaMnO₃, FeO |
| High symmetry | Smooth D3 variation → smaller error | NiO, IrO₂ |
| Dense packing | Reduces artificial dip | Rutile oxides |

Effect of ionic size and oxidation state

Large ions such as La³⁺ and Sr²⁺ have high polarizability, increasing weak dispersion interactions and resulting in larger D3-induced errors.

Higher oxidation state ions such as Ti⁴⁺, Ru⁴⁺, and Ir⁴⁺ are smaller and more tightly bound, reducing dispersion-related artifacts.

Electronic and geometric effects

LaMnO3contains Jahn–Teller active Mn3+, producing unequal Mn–O bond lengths and strong structural distortion, which explains its highest D3-induced error.

IrO2is an anomaly: despite heavy Ir atoms, it shows the lowest error because its compact rutile geometry dominates over atomic mass effects.

Conclusion

Perovskite>Rock Salt>Rutile

Thus, open, distorted, and highly polarizable structures show the largest D3-induced errors, whereas dense, symmetric, and compact structures show the smallest errors.